Coating Super Wetting Agent RH-T1245

Component:

polyether modified polysiloxane

Character:

A special polyether modified siloxane,which has super wetting properties.It improves the spreading and substrate wetting,especially for non-metal substrate material.To prevent the shrinkage due to the failed wetting.

Specifications:

Appearance	:Colorless to amber transparent oily liquid

Viscosity:60-150cps

Active content:100%
Flash point:	＞100℃

Reflexable index:1.450-1.460

Usage:

Used as the substrate wetting agent for solvent-based,water-based coatings and pinting inks.The recommended dosage is .01-1.0％ of the total fomulations

Packing:

25Kg /200Kg plastic drum/iron drum or according to customer’s request.

Transportation and storage:

Transportation as non-dangerous goods.. Store in cool and ventilated warehouse. 12 months of storage period.