Leveling Agent for Coating RH-T1010

Component:

Aralkyl modified polysiloxane

Character:

- It improves the surface property of solvent-based coatings

- Special with emphasis on very rapidly leveling.

- Differences with most organic silicone auxiliaries,it takes into effect in the form of deforming (i.e. : no foam stabilization),this depends on the polarity of coating systems.

- It is heat resistant .

- It doesn’t give smooth hand feelings.

Specifications:

Appearance	:Colorless to amber transparent oily liquid

Non-volatile content:＞95.0%
Viscosity（25℃）：60-150mm2/s

Refractive Index(25ºC)：1.450-1.460

Usage:

The recommended dosage is 0.1～1.0％ of the total fomulations.

Packing:

25Kg /200Kg plastic drum/iron drum.

Transportation and storage:

Transportation as non-dangerous goods.. Store in cool and ventilated warehouse. 12 months of storage period.