Insulator liquid silicone rubber RH－G603/50

Model        RH－G603/50

Specification

Appearance:                                             A translucent/ B blue-grey

Viscosity(28℃, mpa.s)                                         290000~320000

Operative time after mixture                                     ≥48h(25°C)

Hardness(Shore A)                                              50

Tensile strength (MPa)                                           ≥4.5

Elongation at break (%)                                          ≥300

Tear strength(KN/m)                                             ≥18

Volume resistivity(Ω.mm)                                         ≧1*1015

Relative permittivity (100Hz)                                       ≤3

Dissipation factor                                                 0.002

Tracking resistance, 1A 4.5                                         PASS

Frequency electrical strength(Normal oil,rapid pressurization)( kV/mm)      ≧20

Property

2-components additional liquid silicone rubber, which is produced by addition reaction ,lower viscosity, lower temperature curing, excellent hydrophobicity, high tear strength. Excellent electrical properties. Comfortable operating performance.

Applications

Used for medium and low voltage cable accessories, lightning arrester, the cladding of Vacuum Interrupter, etc.

Use method

The A and B components are supplied strained and de-aired. Mix parts A and B in a 1:1 ratio. Airless mixing, metering and dispensing equipment are recommended for production operations. When parts A and B are mixed,please use in time, the mixture will remain processable for a minimum of 50 hours at 25°C.

Package and Storage

20kg/drum or 200kg /drum. The shelf Life is half a year at normal temperature. Over this period, Samples can be qualified after testing and is still in use.

Attention

Avoid the products contact with the compound containing N,P,S,Sn,etc to prevent damaging the catalyst,otherwise the catalyst will be difficult to cure.