Insulator liquid silicone rubber RH－G605/40

Model        RH－G605/40

Specification

Appearance:                                              A translucent/ B translucent

Viscosity(28℃, mpa.s)                                        2000000~2500000

Operative time after mixture                                     ≥48h(25°C)

Hardness(Shore A)                                              38-40

Tensile strength (MPa)                                           ≥7.5

Elongation at break (%)                                          ≥600

Tear strength(KN/m)                                             ≥20

Volume resistivity(Ω.mm)                                         ≧1*1015

Relative permittivity (100Hz)                                       ≤3

Dissipation factor                                                 0.002

Tracking resistance, 1A 4.5                                         PASS

Frequency electrical strength(Normal oil,rapid pressurization)( kV/mm)      ≧20

Property

2-components additional liquid silicone rubber, which is produced by addition reaction ,high viscosity, lower temperature curing, excellent hydrophobicity, high tear strength. Excellent electrical properties.

Applications

Casing, cable terminal, all kinds of medium and high voltage insulators etc.

Use method

The A and B components are supplied strained and de-aired. Mix parts A and B in a 1:1 ratio. Airless mixing, metering and dispensing equipment are recommended for production operations. The two LSR components are delivered by pumps through a static mixer into the heated mold,the recommended mold temperature is 110-115°C,a wider temperature range 90-130°C is also available. Here the injection pressure measures 80bar. a filling time is better controlled in 120 seconds, it depends on the size of the different products.When parts A and B are mixed,please use in time, the mixture will remain processable for a minimum of 50 hours at 25°C.

The injection pipe can be disassembled and stored in cold storage (but it should not be too long), so it is convenient for the next time to continue to use.

Package and Storage

20kg/drum or 200kg /drum. The shelf Life is half a year at normal temperature. Over this period, Samples can be qualified after testing and is still in use.

Attention

Avoid the products contact with the compound containing N,P,S,Sn,etc to prevent damaging the catalyst,otherwise the catalyst will be difficult to cure.