Zhejiang Runhe Chemical New Material Co., Ltd

Add: Rm.1906, Guangli Mansion, No.136, Qingchun Road, Hangzhou, Zhejiang, China

Tel: +86-571-85092338   Fax: +86-571-87246635

Specification

【Product Name】Levelling Agent for Coating RH-T1006

【Component】Polyether modified polysiloxane

【Instruction】

It can increase the wetting property of the bottom materials and anti-cratering property by decreasing the surface tension of the coatings. It increases the smoothness of surface, scratch resistance and anti-adhesive property, improves the acceptance of dust and spray and it make the certain thickness in upright level.  It decreases the air sensitive of wood paint and furniture paint and prevents Bernard swirl. And it improves the orientation of flatting agent.

【Basic Character】

Appearance	: Colorless to amber transparent oily liquid

Non-volatile content: 12-13%

Solvent: Dimethylbenzene/ Ethylene glycol phenyl ether

【Usage】

The recommended dosage is 0.1～0.5％ of the total formulations, it is added at any stage of production and also can be added after the production.

【Package】

180Kg, or 25Kg/Plastic barrel

【Storage】

Store in cool and ventilated warehouse. 12 months of storage period.