Phenyl Hydrogen Silicone Resin RH-SH303-2B

Main content  Phenyl Hydrogen Polysiloxane

Specifications

Appearance: Colorless to light yellow transparent liquid

Viscosity:（25℃,mPa.s）:6500-6800

Volatile content（150℃/3h）:≤1.0%

Refractive index: 1.5250~1.5400

Hydrogen content（wt%）:0.22-0.25%

Character

Used as the curing agent of LED rubber and Electronic and electric encapsulation rubber.  It has good intermiscibility with phenyl vinyl silicone resin,no effect on the refractive index and the light transmittance.

Application

1. It is used in LED and the encapsulation of the Electronic and electrical components for moisture-proof, anti-dust,corrosive proof,shock resistance,and sealings,and for the increasement of service performance and parameter steadiness.

2. Insullac：impregnated coil;impregnated glass colth and casing pipe;bonded mica insulation,electronic element protection.

Attention

Store in a cool dry place, tightly closed.,avoid the moisture in the air.

Avoid the N、P、S、Pb, tin , cadmium , mercury and heavy metal.

Avoid stored together with soda, a strong oxidant.