Phenyl Vinyl Silicone Oil RH-SP0503

Main content  Phenyl Vinyl Linear Polysiloxane

Specifications

Appearance: Colorless to light yellow transparent liquid

Viscosity:（25℃,mPa.s）:1500

Volatile content（150℃/3h）:≤1.0%

Refractive index: 1.5150~1.5350

Vinyl content（wt%）: 1.3%

Character

It contains branched phenyl vinyl silicone oil and vinyl group. It has good reaction activity in the hydrosilylation reaction. It can achieve better reinforcement effect when used in phenyl silicone gel.

Application

Used in the encapsulation of LED and the Electronic and electrical components. It has high transmittance when together used with phenyl hydrogen silicone resin and phenyl vinyl silicone resin,To make low hardness LED encapsulants,silicone gel or fix electronic components.

Attention

Store in a cool dry place, tightly closed. One year storage period and transport as non-dagnerous goods. avoid the moisture in the air.

Avoid the N、P、S、Pb, tin , cadmium , mercury and heavy metal.

Avoid stored together with soda, a strong oxidant.