Phenyl Vinyl Silicone Oil RH-SP606-2

Main content  Phenyl Vinyl Polysiloxane

Specifications

Appearance: light yellow transparent liquid

Viscosity:（25℃,mPa.s）:7000-9000

Volatile content（150℃/3h）:≤1.0%

Refractive index: 1.5250~1.5290

Vinyl content（wt%）: 5.17%-5.38%

Character

The reliability of LED is 30% decided by the chip and 70% decided by the encapsulation. The Phenyl Vinyl Silicone Resin is used in LED and the encapsulation protection of the Electronic and electrical components. High cured film hardness,good light transmission,low light decay,good anti-yellowing and ageing-resistance,low shrink and small moisture absorption rate;It has excellent adhesion to PPA,PCB,electrical components,ABS,metal. Excellent mechanical and  electrical insulating property.Super heat stability. Good solvent and water resistance,anti-ablative and radiation resistance.

Application

1.Used in the encapsulation of LED and the Electronic and electrical components for moisture-proof, anti-dust,corrosive proof,shock resistance,and sealings,and for the increasement of service performance and parameter steadiness.

2.Insullac:impregnated coil;impregnated glass colth and casing pipe;bonded mica insulation,electronic element protection.

Attention

Store in a cool dry place, tightly closed. One year storage period and transport as non-dagnerous goods. avoid the moisture in the air.  Avoid the N、P、S、Pb, tin , cadmium , mercury and heavy metal.  Avoid stored together with soda, a strong oxidant.