Silicone Leveling agent RH-T308

Product Name:  Silicone leveling agent for coatings RH-T308

Component:Polyether modified polysiloxane

Instruction:

It can increase the wetting property of the bottom materials by decreasing the surface tension of the coatings. It improves the smoothness of surface, scratch resistance and anti-adhesive property, improves leveling,gloss, and Orientation of pigment and filler. Applied as additives in solvent-based, solvent-free based and water-based paint system.

Basic Character

Appearance	: Colorless to amber transparent oily liquid

Viscosity:500-1000cps
Refractive index: 1.4400-1.4500

Usage

The dosage is depended upon the type of formulations,solvent,resin and the total solid content .The recommended dosage is 0.1～1.0％ of the total formulations.

Generally,it is added during the grind or the paints preparing,or be post-added..

A thorough application test is necessary to get an ideal result.

It has different charateristics when used in different systems.

It is sometimes cloudy at low temperature,that will not affect on the quality. The cloudy will disappear by heat.

Package:200Kg, or 25Kg/Plastic barrel

Storage:

Transportation as non-dangerous goods

Store in cool and ventilated warehouse. 24 months of storage period.