Silicone rubber adhesion accelerator RH-GZ-03

Introduction

1.This product is colorless transparent compound, low viscosity liquid.

2.It can efficiently increase the adhesion of base materials as added into addition type silicone rubber.

Using method

Mix proper amount of it with silicone bubber,stir evenly, RH-GZ-03 contains 4.1%~4.2% vinyl functional groups, The operator need to consider the formula of Si-H ratio, so that it does not affect the curing character.  Dosage: 1~3%.

Package

1kg/plastic bottle or 5kg/plastic bottle , storage for 3 months in room temperature.

Storage and attention

1.Store in room temperature or in low temperature.

2. Cover the bottle immediately after using, to avoid destroying the quality.

3. Avoid the products contact with the compound containing N,P,S,Sn,etc  ,and avoid long term exposure in air and avoid moisture and water which will affect its adhesion.

4. Avoid sunniness