Silicone spreading and penetrating agent RH-209

Product Name： Silicone spreading and penetrating agent RH-209

Introduction:

Silicone spreading and penetrating agent RH-209 is a modified trisiloxane, and is an organic silicone surfactant with super ability of spreading. It makes the water surface tension lower down to the 20.5mN/m at the concentration of 0.1%(wt.).

Feature：

Super spreading and penetrating agent.

Low surface tention,

High cloud point.

Nonioic.

Character:

| Appearance | Colourless to light amber liquid |
| --- | --- |
| Viscosity（25℃，mm2/s） | 20-40 |
| Surface tension（25℃，0.1%，mN/m） | <21.0 |
| Cloud point（1% wt，℃） | >35℃ |
| Remarks | It is sometimes cloudy and frozen at low temperature,that will not affect on the quality. The cloudy will disappear by heat. |

Use Area :

- 1. Used in agrochemicals.

- Used as spray adjuvant:RH-209 can increase the coverage of the spraying agent,promote the uptake and decrease the dosage of the spraying agent.The RH-209 is the most effective when spray mixtures are (i) within a PH range of 6-8,and (ii) prepare the spray mixture for immediately use or within 24h preparation.

Used in agrichemical formulations: RH-209 can be added in the original pesticide.

- Used in coatings and paints:

- RH-209 can be widly used in water based and solvent based coatings and paints.It is  effective at the very low use level,it is a super wetting and penetrating agent especially used in water based coatings and paints. It provides low surface tension and high surface activities,improves the flow,leveling,smoothness and wetting of the base materials,etc.

- The dosage is depended upon the type of formulations.

- The recommended dosage is 0.1～0.2％ wt% of the total water based systems and 0.5% of the total solvent based systems.

- A thorough application test is necessary to get an ideal result.

- It has different charateristics when used in different systems.

Package：200Kg, 1000Kg, or 20Kg plastic barrel,or up to clients request.

Storage：Store in dry place, avoid exposing to the sun.

Valid Period: 2 years

Transport on no-danger cargoes