Liquid silicone rubber for Screen Printing RH-G8

Model        RH-G8

Introduction

Transparent two component addition type liquid silicone rubber has good weather resistance, small shrinkage, good size stability, good adhesion with the cloth. It can adhere to natural and synthetic fabrics surface firmly through screen printing. The printed words and pattern has good third dimension, as well as excellent washing resistance, and peeling strength,bight,matt,semi-matt appearance, on-stick feel; Non-toxic, easy to use, water proof,non-slip,anti high and low temperature. It is an excellent alternative of PVD (plastisol), PU, and PA resins. It has water proof, skid-proof, breathe freely, anti high and low temperature property.

This product can form in one piece to be made into given thickness round angle products.

Application

Widely used in non-slip and heat insulation for gloves.

Specification

A                        B

Viscosity（25℃）mpa.s              1400000~1700000		      3000~5000

Mixing proportion                      10		 		          1

Curing temperature ℃                             80~150

Hardness  ShoreA                                40~42

Tensile Strength MPa                               ≧5.5

Elongation %                                     ≧500

Tearing strength  ，KN/M                          ≧22

Using method

Mix A and B at a rate of 10:1 in container, stir quickly to even. Vacuum degassing. but generally the bubble will self-disappear during the printing. Prepare for immediately use according to the dosage. Start from small dosage to know the using skill. Recommend using fine screen mesh(>=120 meshes) to get smooth printing effect.

We can also adjust the operation time and curing time according to client’s demand. The other specifications can be adjusted according to client’s request.

Storage and attention

1. Avoid the products contact with the compound containing N,P,S,Sn,etc

2. Avoid moisture which will reduce the lifetime.

3, Validity period is more than 6 months, it can be used after the validity period if the test result is up to the standard.

Package

20kg plastic drum. Transport as non-dangerous goods.