Liquid silicone rubber for Scutcheon RH-G3

Model        RH-G3

Introduction

Transparent two component addition type liquid silicone rubber. Good weather resistance, small shrinkage, good size stability, good adhesion with the cloth. Widely used in the production of clothing scutcheon. The printed letters and patterns has good sense of three-dimension. Non-stick feel; Moderate viscosity, easy to use, middle temperature rapid curing, also has excellent peel strength, abrasion resistant, bright. Environmental and non-toxic. It is an excellent alternatives of PVD (plastisol), PU, and PA resins.

Application

Clothing scutcheon, clothing patterns, Scutcheon of sports gloves, handbags, travel bags, luggage, etc.

Specification

A                        B

Viscosity（25℃）mpa.s              100000~120000		      3000~5000

Mixing proportion                      10		 		          1

Curing temperature ℃                             80~150

Hardness  ShoreA                                36~38

Tensile Strength MPa                               ≧6

Elongation %                                     ≧350

Tearing strength  ，KN/M                          ≧15

Using method

Mix A and B at a rate of 10:1 in container, stir quickly to even. Vacuum degassing. Prepare for immediately use according to the dosage. Start from small dosage to know the using skill.

Storage and attention

1. Avoid the products contact with the compound containing N,P,S,Sn,etc

2. Avoid moisture which will reduce the lifetime.

3. Validity period is more than 6 months, it can be used after the validity period if the test result is up to the standard.

Package

20kg plastic drum. Transport as non-dangerous goods.