Liquid silicone rubber for Socks RH-G10

Model        RH-G10

Introduction

The product is transparent two component addition liquid silicone rubber. It can adhere to natural and synthetic fabrics(elastic fabrics) surface firmly through screen printing. The printed words and pattern has good third dimension, as well as excellent washing resistance, and peeling strength.

Completely non-toxic, easy to use. Soft and comfortable health care.

Application

Used for sock bottom screen printing, Non-slip, massage function.

Specification

A                        B

Viscosity（25℃）mpa.s              ＞600000		          3000~5000

Mixing proportion                      10		 		          1

Curing temperature,℃                             80~150

Hardness,ShoreA                                 37~40

Tensile Strengt, MPa                               ≧6

Elongation, %                                    ≧300

Tearing strength,KN/M                              ≧18

| Model | Mix Ratio A:B | Viscosity（25℃）mpa.s A/B | After curing |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Hardness（Shore A) | Tensile Strengh, MPa | Elongation, % | Tearing strength,KN/M |
| RH-G10-high viscosity | 100:2 | 800000-900000/500 | 23-25 | ≥4 | ≥700 | ≥10 |
| RH-G10-middle viscostiy | 100:2 | 150000-200000/500 | 23-25 | ≥4 | ≥700 | ≥10 |
| RH-G10-low viscosity | 100:2 | 50000-60000/500 | 23-25 | ≥4 | ≥700 | ≥10 |

Note: It will have certain influence on the adhesive property when the curing temperature is less than 100 ℃.

Using method

Mix A and B at a rate of 10:1 in container, stir quickly to even. Vacuum degassing. but generally the bubble will self-disappear during the printing. Prepare for immediately use according to the dosage. Start from small dosage to know the using skill.

We can also adjust the operation time and curing time according to client’s demand. The other specifications can be adjusted according to client’s request.

Storage and attention

1. Avoid the products contact with the compound containing N,P,S,Sn,etc

2. Avoid moisture which will reduce the lifetime.

3, Validity period is more than 6 months, it can be used after the validity period if the test result is up to the standard.

Package

20kg plastic drum. Transport as non-dangerous goods.