Liquid Silicone Rubber for Textile Belt RH-G2

Model        RH-G2

Introduction

Transparent two component addition type liquid silicone rubber, which has good weather resistance and good adhesive force. The printed words and pattern has good third dimension, as well as excellent tensile strength, elongation and anti-tearing strength; Washing resistance, and abrasion resistant. Non toxic, easy to use.

Application

Used for the logo sign coating on trimming ribbon (such as elastic belt), printing ribbon of sports suit, children’s clothing and logo sign on bootlace, the pattern on packaging ribbon or the anti-slip purpose of underwear..

Specification

A                        B

Viscosity（25℃）mpa.s              90000~11000		      3000~5000

Mixing proportion                      10		 		          1

Curing temperature ℃                             80~150

Hardness  ShoreA                                30~33

Tensile Strength MPa                               ≧6

Elongation %                                     ≧420

Tearing strength  ，KN/M                          ≧19

Using method

Mix A and B at a rate of 10:1 in container, stir quickly to even. Vacuum degassing. but generally the bubble will self-disappear during the printing. Prepare for immediately use according to the dosage. Start from small dosage to know the using skill. Recommend using fine screen mesh(>=120 meshes) to get smooth printing effect.

We can also adjust the operation time and curing time according to client’s demand. The other specifications can be adjusted according to client’s request.

Storage and attention

1. Avoid the products contact with the compound containing N,P,S,Sn,etc

2. Avoid moisture which will reduce the lifetime.

3, Validity period is more than 6 months, it can be used after the validity period if the test result is up to the standard.

Package

20kg plastic drum. Transport as non-dangerous goods.